## Slide 1
Molten Glass Energy Storage Reservoir
Halotechnics GameChanger Stage Gate Review
Dr. Justin Raade, CEO and Founder
Matt Jonemann, Engineering Manager
December 17, 2014
www.halotechnics.com

## Slide 2: Phase 1 work: Heat pump
Waste
Heat
Electricity
Motor
compress
expander
Generator
steam turbine
400 °C
200 °C
air in
air out
High Quality Heat Stored

## Slide 3: Phase 1 work: Commercial feasibility

## Slide 4: Phase 1 work: Conclusions
Equipment needed for high temperature heat pump is technically feasible but not commercially available
Reducing cost is #1 priority in energy storage market
Electrical resistive heater and molten salt energy storage has near-term commercial opportunities
Molten glass energy storage may further reduce storage cost

## Slide 5: A new energy storage platform
Molten glass enables new energy storage platform
  Inherently cheap storage material (low $/kWh)
  4x storage density vs. molten salt (high kJ/L)
New storage applications
  Low cost electrical energy storage
  Greater flexibility in gas turbines by storing heat at full combustion gas temperature
  Low carbon steam production
Charging
Electrical energy
Combustion
Discharging
Molten salt
Air
Steam

## Slide 6: Integrate into existing thermal power plants
Generator
Steam Turbine
SteamBoostTM
(molten salt)
HeatBoostTM
(molten glass)
FireBoostTM
(molten glass, TBD)
50 °C
95 °C
600 °C
1600 °C
Generator
Gas Turbine
Heat Recovery Steam Generator
540 °C
Inject heat further upstream:
Higher temperature (higher efficiency, higher energy density)
Leverage more existing equipment (lower capex)
Typical combined cycle power plant with heat injection points

## Slide 7: Showstoppers to molten glass energy storage
 | Showstopper |  | Solution
1. | Pumpable glass manufactured cost too high |  | Use soda lime glass, Na2O-CaO-SiO2, ~$200/ton
2. | No practical containment material |  | Use zirconia ceramics, proven for years with soda lime glass
3. | No interface to power block |  | Control heat release with salt or air, no glass pumping
Halotechnics has unique capabilities and can build on previous experience to develop practical molten glass energy storage
Lessons learned from previous work with phosphate and vanadium based glasses

## Slide 8: Molten glass energy storage reservoir
Tank Shell
Refractory Lining
Ceramic Insulation
Molten Glass
Electrode Heaters
Air Outlet
Air Inlet
Patent pending

## Slide 9: Market driven design
Decentralized generation (20-50 MW) is the correct size for procurement
  Utilities have built hundreds of natural gas peaker plants in this size range
Sufficient discharge profile (4 hours duration on 3 consecutive days) to qualify for “capacity payments”
  Utilities pay for standby power, available upon demand.
  Typical payment is in $/kW-month regardless of hours of operation
Use the minimum required storage output duration
  Reduces capex required to qualify for capacity payments
Plant must last >10 years for good project economics
Commercial viability requires 20-50 MW, 4 hours storage plant with minimum 10 year life

## Slide 10: Dimensions and storage capacity
22 m
22 m
Glass reservoir sized for 2000 ton inventory (common in glass industry)
Square footprint (22 m x 22 m) to reduce surface area and cost
1.8 m (72”) glass pool depth is feasible with standard furnace designs
1.8 m
At target ΔT of 500 °C, design can store 400 MWht, enough for
40 MWe, 4 hours storage
Front View
Top View
Base-case design:

## Slide 11: Base-case design: Process flow diagram
Patent pending

## Slide 12: Capital cost budget
Given revenues from capacity payments and estimated O&M costs, how much capital cost can we allow and still achieve an acceptable IRR?
Molten glass shows promise as commercially viable energy storage technology
Assumptions:
40 MW, 4 hours storage
Glass inventory: $0.4 million
Soft costs (project development, permitting): 5% capex
O&M costs: 2% capex annually
Rebuild furnace every 10 years
$10/kW-month capacity payments
Target 10-15% IRR requires furnace costs <$25-30 million

## Slide 13: Differentiated solution
SteamBoostTM
(molten salt)
HeatBoostTM
(molten glass)
Credit: Bloomberg New Energy Finance, 2014
Molten glass enables differentiated technology roadmap

## Slide 14: Technical challenges
Glass properties suitable for storage
  Inherently low cost and stable
Charging
  Electrode heater power
  Electrode heater lifetime
Storing
  Heat losses through tank walls
Thermal cycling
  Thermal shock to refractories
  Thermal expansion of tank
Discharging thermal energy from glass
  Achieving high heat flux
  Controlling discharge rate
  Heat transfer to power block



!
!
Risk Profile:
Feasible
Need GameChanger!

!

## Slide 15: Glass properties
Glass cullet (sorted, recycled glass) available in millions of tons annually at <$200/ton
Want low-iron clear glass for better radiative heat transfer from bulk (<0.1% Fe2O3)
Glass could be used as a stable, low-cost thermal energy storage media
Property | Value
Typical composition by weight (soda lime window glass) | 73% SiO2, 14% Na2O, 9% CaO, 4% MgO, 0.15% Al2O3, 0.1% Fe2O3
Heat capacity (Cp) | 1.45 kJ/kg-K
Density (ρ) | 2300 kg/m3
Maximum temperature stability (alkali volatilization) | 1500-1600 °C
Softening point | 700-800 °C
Typical clear glass cullet


## Slide 16: Charging
Molten glass is a good electrical conductor
Electric glass melting furnaces up to 300 tons/day in commercial use
Molybdenum electrode heaters can last for entire furnace campaign (7-10 years)
It is feasible to achieve 40 MW heating power or more with standard electrodes


## Slide 17: Storing: heat losses through tank walls
Assume 2000 ton glass inventory (size of large commercial float glass furnace)
Thin AZS refractory layer for corrosion resistance
~18” firebrick layer for low-cost, resilient insulation. Forms “self sealing” cold zone
Steel shell for structural strength
Additional external insulation to reduce heat losses
Molten Glass
AZS refractory
Steel shell
Air
1500 °C
25 °C
Tank temperature
Firebrick
Insulation
Air
Tg
T1
T3
T4
T6
Ta
It is feasible to achieve <5% heat losses per day with standard insulating materials
T2
T5
<0.6 kW/m2 heat losses


## Slide 18: Thermal cycling
Refractories can typically withstand some thermal swings, for example due to idling a furnace over the weekend
High temperature ramp rates result in higher stresses
ASTM standard for thermal shock resistance measures strength after repeated, rapid cycling from 1200 °C to room temperature
  Too severe to predict behavior for our system
Must verify that refractory can withstand 2000 thermal cycles (10+ year life)
!

## Slide 19: Refractory thermal cycling and corrosion tests
Test thermal cycling first, then corrosion resistance (will be a trade-off)
  Chromia (Cr2O3), zirconia (ZrO2), and alumina (Al2O3) fused-cast refractories are most corrosion resistant
  Sintered refractories are most shock resistant
  Can tailor composition and manufacturing process to achieve better overall performance
Test refractory samples in lab furnace
  Thermal cycling: 6 cycles per day, repeat ~200x for 1 year accelerated life
  Corrosion: Isothermal test with glass
  Assess mechanical strength and/or corrosion rate of samples
Select refractories with guidance from commercial vendors
  Durital, Monofrax (RHI)
  Zirchrome (Saint-Gobain SEFPRO)
1500 °C
1000 °C
4 hrs
Thermal cycling profile
Refractory samples after 1500 °C corrosion test (courtesy RHI)

## Slide 20: Discharging: adequate heat flux
Target 100 MWt heat transfer rate from glass to meet 4 hr discharge spec
Requires ~200 kW/m2 from glass pool
  Easier at 1500 °C. Harder at 1000 °C.
Must promote good convection
  Bubblers
  Convoluted flow path
  Turbulent flow
Must promote good radiation
  Use clear (low iron) glass
Must verify ability to achieve 4-8 hour discharge times with reasonable furnace geometries
!
>200 kW/m2 heat transfer

## Slide 21: Thermal design and modeling
Verify key performance metrics via iterative design and modeling
  Heat discharge rate
  Heat losses
  Thermal expansion of refractories
Leverage existing regenerator designs for cooling air flow
Optimize glass pool depth for tradeoff between heat losses and discharge performance
Mature modeling software available from glass industry
Refractory checker-brick regenerator

## Slide 22: Budget and timeline
$425,000 budget, 8 month project in two phases
  Phase 2: $250,000. Refractory thermal testing and system design.
  Phase 3: $175,000. Corrosion testing, thermal modeling and design iteration.
 | Phase 2 |  |  |  | Phase 3 |  |  | 
Task or Milestone | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8
1. Thermal cycling testing of refractories |  |  |  |  |  |  |  | 
Refractory selection with guidance from established vendors |  |  |  |  |  |  |  | 
Develop test methodology (ramp rate, soak time, temperatures) |  |  |  |  |  |  |  | 
Perform thermal cycling tests |  |  |  |  |  |  |  | 
Evaluate results. Verify that some candidates survive intact. |  |  |  |  |  |  |  | 
2. System design |  |  |  |  |  |  |  | 
System specifications based upon market need |  |  |  |  |  |  |  | 
Preliminary design |  |  |  |  |  |  |  | 
Toll Gate: Thermal cycling pass, preliminary design feasible |  |  |  |  |  |  |  | 
3. Corrosion testing of refractories |  |  |  |  |  |  |  | 
Refractory downselection with candidates from previous phase |  |  |  |  |  |  |  | 
Develop test methodology (ramp rate, soak time, temperatures) |  |  |  |  |  |  |  | 
Perform corrosion tests |  |  |  |  |  |  |  | 
Evaluate results. Verify that some candidates survive intact. |  |  |  |  |  |  |  | 
4. Thermal modeling to verify desired charge and discharge rates |  |  |  |  |  |  |  | 
Build model based upon design developed in previous phase |  |  |  |  |  |  |  | 
Vary parameters (flow path, gas composition, gas velocity) |  |  |  |  |  |  |  | 
Iterate design and verify desired discharge rate |  |  |  |  |  |  |  | 
5. Final report to document results of experimental work and modeling |  |  |  |  |  |  |  | 
Toll Gate: Corrosion test pass, sufficient discharge rate feasible |  |  |  |  |  |  |  | 

## Slide 23: Follow on plan
Pilot plant with strategic partners at location TBD
Typical utilities require minimum of 1 MW plant with 1 year of operational data to be considered “proven technology”

## Slide 24: Extra slides

## Slide 25: Outline
Halotechnics overview
Market need for storage
Summarize Phase 1 results
Molten glass energy storage
Technical risks are real but can be mitigated with GameChanger project

## Slide 26: Halotechnics, Inc. – Corporate Profile
Halotechnics: An industrial technology company focused on molten salt and molten glass systems
  We offer engineering design services, equipment, and proprietary salt materials to our customers
  Founded in 2009 as a spin-out of Symyx Technologies (SMMX), the pioneer of high throughput chemistry
  22,000 salt mixtures screened to date, patents filed on novel materials and system designs
Financing
  $6.5 million in federal grants from NSF, DOE, NREL, and ARPA-E (2009-2014)
  $1.05 million subcontract from Alcoa (2014-2016)
  $1.5 million contract from CEC pending (2015-2017)
Organization
  Headquartered in Emeryville, California
  12,000 square foot chemistry and engineering labs
  12-person team with molten salt and energy experience (engineers, chemists, power sector professionals)
Low cost energy storage is the key to abundant clean energy
Select Partners and Customers

## Slide 27: Halotechnics Product Markets
Halotechnics Thermal Fluids Platform
Energy
Waste Heat Recovery
Thermal Electricity Storage
Glass manufacturing
Heavy oil upgrading
Renewable peaker plant
Steel manufacturing
Reliable
wind power
In-situ oil shale conversion
Aluminum
smelting

## Slide 28: Halotechnics Products
Saltstream and Haloglass
Enabling a new class of applications in extreme heat
www.halotechnics.com/products
Halotechnics products were developed by screening over 23,000 unique mixtures
We aim to deliver value-driven products from industrially available chemicals.

## Slide 29: Broad experience with glass at Halotechnics
High throughput glass chemistry screening
Graphite piping from molten glass test loop after testing at 1100 °C
Proprietary vanadium-based glass
Proprietary phosphate-based glass
(a)
(b)
(d)
(c)

## Slide 30: Experience with molten salt systems
5 kW
5 kW
HOT TANK
Pilot scale 700 °C molten salt thermal storage system (30 kWh, 2,000 kg salt, proprietary chloride composition)
Funded by $1 million NREL SunShot Incubator award (2012-2013)
Executed aggressive 15 month project schedule, from design to experimental data
Notes: Halotechnics is developing the complete engineering solutions for thermal storage systems in addition to the materials science development of the fluids

## Slide 31: Renewable energy needs electricity storage
20,000
22,000
24,000
26,000
28,000
30,000
32,000
34,000
36,000
38,000
40,000
42,000
44,000
46,000
0:00
1:30
3:00
4:30
6:00
7:30
9:00
10:30
12:00
13:30
15:00
16:30
18:00
19:30
21:00
22:30
0:00
Electricity
Demand (MW)
12,000 MW of storage is needed in California alone
Time of Day (2020 projected load)
12,000 MW
From Storage
Demand minus solar and wind

## Slide 32: Gathering momentum for storage

## Slide 33: Our competition cannot meet the need
Pumped hydro – can’t site it
Compressed air –
can’t site it
Peaker plants – CO2, NOx pollution
Batteries –
too expensive

## Slide 34: Phase 1 work: Down-selected plant schematic
Electricity
Generator
steam turbine
565 °C
290 °C
Charging
Discharging
Waste heat (optional)

## Slide 35: Charge
Initial charge: glass at 1000 °C
Charge via electrode heaters immersed in glass

## Slide 36: Store energy
Fully charged.
Glass at 1500 °C

## Slide 37: Initial discharge
Discharge via convective and radiative heat transfer to cooling gas
Add bubblers in glass to reduce stratification
Must control gas outlet temperature
Target air outlet temp: 600 °C

## Slide 38: Final discharge
Fully discharged.
Glass returns to 1000 °C

## Slide 39: System layout
Air Intake
Generator
Steam Turbine
Energy storage
Heat transfer
Energy conversion
Energy can be delivered with air to the power block for electricity generation
Blower
Air Outlet
Boiler
Electricity In
Electricity Out

## Slide 40: Budget justification
Aggressive project scope and timeline requires staffing of experienced professionals
  0.4 FTE Project Manager (thermal/mechanical engineer)
  0.4 FTE Staff Scientist (chemist)
  0.2 FTE CEO (system architecture, techno-economic analysis)
Item | Description | Cost
Direct Labor | labor rates | $70,500
Overhead and Fringe Benefits | rent, legal, patents, SG&A, benefits | $70,500
Materials and Supplies | refractory samples, glass samples | $4,000
Equipment | N/A | $0
Travel | visit glass engineering firm, glass modeling firm, test lab | $10,000
Consultants | glass chemistry, test method development | $6,000
Subcontracts |  | $264,000
Thermal cycling test lab |  | $53,000
Glass engineering firm |  | $94,000
Glass corrosion test lab |  | $57,000
Glass modeling firm |  | $60,000
TOTAL ($) |  | $425,000

## Slide 41: Market-driven deliverables
Note: Technical deliverables above are for base-case design: 40 MW, 4 hour storage plant with a glass pool 22 m x 22 m x 1.8 m, operating between 1500 °C max and 1000 °C min
Commercial Requirement | Technical Deliverable | Phase
Decentralized power generation | Design plant with 20-50 MW rated power | Phase 2
>10 year plant life | At least one commercially available refractory suitable for lining the glass reservoir. Suitability is defined as less than 50% loss of strength (as measured by the modulus of rupture) after 200 thermal cycles. | Phase 2
>10 year plant life | A wall design that can tolerate repeated thermal expansion cycles | Phase 2
<10 hour charge duration | Electrode heater arrangement that can charge glass inventory with >40 MW of heating power | Phase 2
>10 year plant life | At least one commercially available refractory suitable for lining the glass reservoir. Suitability is defined as less than 10 mm/year measured corrosion rate. | Phase 3
4 hour discharge duration | Adequate heat flux from the glass during discharge in order to achieve a discharge duration of four hours (defined as >200 kW/m2 heat transfer rate from glass surface at maximum and minimum operating temperatures of glass) | Phase 3

## Slide 42: Plant lifetime
Assume plant with following dispatch profile (similar to natural gas peaker plants)
  Every day in the spring months: Mar, Apr, May  90 days
  Every day in fall months: Sep, Oct, Nov  90 days
  Once every 7-10 days in other months:  20 days
Typical year sees 200 days of use. Therefore 10 year life requires an estimated 2000 charge/discharge cycles

## Slide 43: From spec, to design, to model
Halotechnics to perform:
  Energy storage market knowledge and customer outreach
  Refractory testing method development and glass selection
  System specification (design concept, footprint and tank sizing, PFD)
Tentative subcontracts:
  Mo-Sci (refractory thermal cycling and corrosion testing)
  TECO (preliminary design based upon spec)
  Glass Service (thermal modeling based upon preliminary design)
System specification
Preliminary design
Thermal modeling
Validated design
Market constraints
Iterative feedback
Available refractories

## Slide 44: SteamBoost project potential
Data obtained from http://GlobalEnergyObservatory.org/
Deploy SteamBoost and HeatBoost at plants nationwide
1100 MW of boost potential in California
10,000 MW nationwide